## Slide 2: Machine Learning for Microstructural Characterization of Archeological Specimens from XRT
Daniela Ushizimaa,b, Ke Xuc, Matthew McCormickd, Dula Parkinsone, Paulo Monteiroc,f
a Computational Research Division, Lawrence Berkeley National Laboratory, Berkeley, CA 94117, USA b Berkeley Institute for Data Science, University of California Berkeley, Berkeley, CA 94117, USA c Civil and Environmental Engineering, University of California Berkeley, Berkeley, CA 94117, USA
d Kitware Inc., Carrboro, NC 27510, USA e Advanced Light Source, Lawrence Berkeley National Laboratory, Berkeley, CA 94117, USA
f Materials Science Division, Lawrence Berkeley National Laboratory, Berkeley, CA 94117, USA

## Slide 3
Ancient Roman Concrete - Pompeii

## Slide 4
Jackson et al., American Mineralogist, Volume 98, pages 1669–1687, 2013

## Slide 5
Notes: Rome was not built in one day but it was built to last.

## Slide 6
Concrete industry faces tough challenges because of its large carbon footprint.

## Slide 7: Environmental Impact
Portland cement: 1866 Coplay Cement Company
Cement industry generates
3 billion ton of CO2
Courtesy: prof. Paulo Monteiro
Source: https://www.engr.psu.edu/ce/courses/ce584/concrete/library/materials/History/DevelopementofPC-main.html
Notes: Production of cement is responsible for 7% CO2 production in the world
Development of Portland Cement in the United States
In the spring of 1866, David O. Saylor, Esias Rehrig, and Adam Woolever started the Coplay Cement Company. The Coplay Cement Company was located along the west side of the Lehigh River and along side of the Lehigh Valley Railroad (L.V.R.R). Early in the 1870’s, Sailor began to experiment with the manufacturing of portland cement from rocks from his own quarry. With this experimentation, Saylor discovered the possibility of making portland cement from raw materials at his disposal. He noticed that the harder burned portions of his Rosendale clinker produced cement that would show a tensile strength equal to that of the best imported portland cement, for a short period of time. However the cement had the problem of crumbling away with time. This problem was do to the raw materials not being properly proportioned.

## Slide 8: World demand/year
Mehta & Monteiro, fourth edition, 2014
Concrete: 33 billion ton
Water: 2.7 billion ton
Aggregate: 27 billion ton
Cement: 3.7 billion ton

## Slide 9: Recent Portland cement production
million metric tons of cement
Courtesy: prof. Paulo Monteiro
Notes: From 800 to 4,000 in 20 years

## Slide 10: Sustainability
Goal:
Eliminate 1.5 billion metric tons of CO2
Challenge:
More than1.5 billion metric tons of alternative material
Supply:
- 607-670 million tons of fly ash
- 220 million tons of slag
Courtesy: prof. Paulo Monteiro
Notes: This research promises to make us rethink how to choose materials for construction in face of climate change and excess of pollutants – can we use fly ash and slag in a larger scale? We are investigating structure of materials being used for millenniums as part of deploying new materials

## Slide 11
Concrete from Harbors
Jackson et al., American Mineralogist, Volume 98, pages 1669–1687, 2013
Specimens acquired from ancient Roman concrete seawater structures in the bay of Pozzuoli (Baiae);
65BC: samples were around 0.85 m below the surface of the breakwater;
Now lies 3.45 m below present sea level, and they are composed of volcanic ash, lime, seawater, and volcanic rocks.

## Slide 12: X-Ray Tomography (XRT)
Notes: We need a method of data analysis and categorization that can be applied to all beamlines.

## Slide 13: Data acquisition
20mm
A
B
C

## Slide 14: Computer Vision Flowchart :
Slicing &
3D rendering
Binarization &
MaxProjection
Masking
Superpixel
Phase segmentation
Segmentation
auditing
Metrology
Enhancement
Vesselness & Texture
Observatory
Discriminatory
Explanatory
Notes: getFiberROI = edge
getProbFibers = Euclidean distance transform
probeDetails =
AHPCS = allylhydridopolycarbosilane

## Slide 15: Rendering of XRT from Baiae samples
Ushizima et al, Materials Research Society 2020

## Slide 16: Partial volumes after segmentation
%Volume | Matrix | Aggregate | Pore | Background
S1 | 35.80 | 15.88 | 0.82 | 47.5
S2 | 35.89 | 29.60 | 13.10 | 21.40
Phase segmentation estimates using Random Forest on full stacks
Ushizima et al, Materials Research Society 2020

## Slide 19
Concrete Imaging from Nanoscale to Microscale
Goal: mechanical resilience and cementitious processes in Ancient Roman architectural mortar – why it outperforms modern concrete?
Neutron
radiography
STEM
tomography
Structure from
in-situ analysis
Hard X-ray
tomography
DVC
Multimodal Data Analysis and Synthesis through Math and ML
Water
absorption
CSH
growth
Concrete
dynamics
Notes: Prof Geosciences at Stony Brook Melissa Sims use APS to study plagioclase deformation.
Overall goal – better concrete! Entire cities around Pompeii, Italy, are still up while our bridges are crumbling and need major repairs every 50 years
Warning: Do not share this as it was not published yet
Multinational Collaboration between USA (LBL ALS, Molecular Foundry, UCB Civil eng, UCB Earth Sciences), Italy (Material Science Dep Univ. Basilicata) and France (Cachan Institute of Technology - Université Paris-Sud) research institutions
Tremsin, Li, Su, Telesca, Marroccoli, de Nigris, Xu, Bouterf, Ushizima, Monteiro, “Neutron measurements of water absorption in cracked and uncracked ancient concrete from Pompeii”, in preparation 2019.
Calcium silicate hydrate (or C-S-H)
This research promises to make us rethink how to choose materials for construction in face of climate change and excess of pollutants – should we address reliance on cement? can we use fly ash and slag in a larger scale? We are investigating structure of materials being used for millenniums as part of deploying new materials

## Slide 20: Cultivating next generation of scientists
Research and development through collaboration with and support to the next generation of scientists and engineers around the world
America, Brazil, Cameroon, Canada, China, India, Kenya, Netherlands, Nigeria, South Africa, Thailand, Tunisia, Zimbabwe
Notes: Ijeoma, Edith, Sam Schickler,

## Slide 21: Acknowledgements
Thank you
http://bit.ly/dxc2020
Prof. Paulo Monteiro
Matt McCormick
Dula Parkinson
Ke Xu PhD student
Dani Ushizima