## Slide 2: Machine Learning for Microstructural Characterization of Archeological Specimens from XRT
Daniela Ushizimaa,b, Ke Xuc, Matthew McCormickd, Dula Parkinsone, Paulo Monteiroc,f
a Computational Research Division, Lawrence Berkeley National Laboratory, Berkeley, CA 94117, USA b Berkeley Institute for Data Science, University of California Berkeley, Berkeley, CA 94117, USA c Civil and Environmental Engineering, University of California Berkeley, Berkeley, CA 94117, USA
d Kitware Inc., Carrboro, NC 27510, USA e Advanced Light Source, Lawrence Berkeley National Laboratory, Berkeley, CA 94117, USA
f Materials Science Division, Lawrence Berkeley National Laboratory, Berkeley, CA 94117, USA

## Slide 3
Notes: Rome was not built in one day but it was built to last.

## Slide 4
Concrete industry faces tough challenges because of its large carbon footprint.

## Slide 5: Environmental Impact
Production 1 ton of cement generates 0.87 ton of CO2
Cement industry generates
3 billion ton of CO2
Courtesy: prof. Paulo Monteiro
Notes: Production of cement is responsible for 7% CO2 production in the world
How much is 3 billion ton of CO2? Just compare with the 5.3 billion ton of CO2 in the US (data for 2013). Or about all the CO2 generated by coal and gas in the US.
Or the amount of pasta eaten in Italy = 3 million tons against the 13 million tons of pasta in the world

## Slide 6: World demand/year
Mehta & Monteiro, fourth edition, 2014
Concrete: 33 billion ton
Water: 2.7 billion ton
Aggregate: 27 billion ton
Cement: 3.7 billion ton

## Slide 7: Recent Portland cement production
million metric tons of cement
Courtesy: prof. Paulo Monteiro
Notes: From 800 to 4,000 in 20 years

## Slide 8: Sustainability
Goal:
Eliminate 1.5 billion metric tons of CO2
Challenge:
More than1.5 billion metric tons of alternative material
Supply:
- 607-670 million tons of fly ash
- 220 million tons of slag
Courtesy: prof. Paulo Monteiro
Notes: This research promises to make us rethink how to choose materials for construction in face of climate change and excess of pollutants – can we use fly ash and slag in a larger scale? We are investigating structure of materials being used for millenniums as part of deploying new materials

## Slide 9
Concrete from Harbors
Jackson et al., American Mineralogist, Volume 98, pages 1669–1687, 2013

## Slide 10
Jackson et al., American Mineralogist, Volume 98, pages 1669–1687, 2013

## Slide 11: Specific chemical goals of project
What is the effect of alumina on the compositions of cementitious phases?
How does the alumina influence the nanoscale bonding environments of the crystalline and poorly crystalline cementitious phases?

## Slide 12: X-Ray Tomography (XRT)
Notes: We need a method of data analysis and categorization that can be applied to all beamlines.

## Slide 13
Concrete Imaging from Nanoscale to Microscale
Goal: mechanical resilience and cementitious processes in Ancient Roman architectural mortar – why it outperforms modern concrete?
Neutron
radiography
STEM
tomography
Structure from
in-situ analysis
Hard X-ray
tomography
DVC
Multimodal Data Analysis and Synthesis through Math and ML
Water
absorption
CSH
growth
Concrete
dynamics
Notes: Prof Geosciences at Stony Brook Melissa Sims use APS to study plagioclase deformation.
Overall goal – better concrete! Entire cities around Pompeii, Italy, are still up while our bridges are crumbling and need major repairs every 50 years
Warning: Do not share this as it was not published yet
Multinational Collaboration between USA (LBL ALS, Molecular Foundry, UCB Civil eng, UCB Earth Sciences), Italy (Material Science Dep Univ. Basilicata) and France (Cachan Institute of Technology - Université Paris-Sud) research institutions
Tremsin, Li, Su, Telesca, Marroccoli, de Nigris, Xu, Bouterf, Ushizima, Monteiro, “Neutron measurements of water absorption in cracked and uncracked ancient concrete from Pompeii”, in preparation 2019.
Calcium silicate hydrate (or C-S-H)
This research promises to make us rethink how to choose materials for construction in face of climate change and excess of pollutants – should we address reliance on cement? can we use fly ash and slag in a larger scale? We are investigating structure of materials being used for millenniums as part of deploying new materials

## Slide 14: What have we learned?
Identification of differences between crystalline Al-tobermorite and poorly-crystalline C-A-S-H in the same cementitious micro-environment.
The coherent, compact fabrics of the Roman maritime concrete structures demonstrate that silicon and aluminum bonding environments in both the Al-tobermorite and the C-A-S-H are sufficiently stable,

## Slide 15: A bit more…
Experimental study of the pozzolanic properties of with lime mixtures should provide important insights into durable and sustainable concrete designs for modern maritime structures.

## Slide 16: Cultivating next generation of scientists
Research and development through collaboration with and support to the next generation of scientists and engineers around the world
America, Brazil, Cameroon, Canada, China, India, Kenya, Netherlands, Nigeria, South Africa, Thailand, Tunisia, Zimbabwe
Notes: Ijeoma, Edith, Sam Schickler,

## Slide 17: Acknowledgements
DAV
Thank you
http://bit.ly/dxc2020

## Slide 18: This is a Title and Content Slide Arial 32 pt
This is text without a bullet. All text is Arial 24 pt. Add or remove bullets with the Bullets button.
  This is a first level bullet. Apply text and bullet levels with the Increase or Decrease Levels List button.
    This is second level text
      This is third level text
  This is a first level bullet
This is text without a bullet. Spacing increases between paragraphs and first level bullets. You can use color or bold sparingly to highlight a word/thought.